SPECIFICATION

The Irish Blood Transfusion Service (IBTS) invite tenders for the supply of gold and silver donor awards in the following categories. Site visits are optional but suppliers are strongly advised to make arrangements to view the existing designs. No discolouration will be accepted.
Gold Drop








9ct Gold Blood Drop Pin

Emblem dimensions: 9ct gold material used should be a minimum size

12mm long x 8mm long x 1.3mm thick

Stem dimensions: minimum 45mm long x .9mm thick

Pin stem to be 9ct soldered to emblem

Minimum weight of finished product (without pin protector) should be at least 1.3 gram

Item should be hallmarked on the reverse of the emblem (not on pin)

Gold plated base metal rubber inserted pin protector should be fitted to the end on each piece


Silver Gilt Pin

Emblem dimensions: minimum size 12mm long x 7.5mm long x 1.2mm thick

Stem dimensions: minimum 45mm long x .9mm thick

Pin stem to be silver soldered to emblem

Minimum weight of finished product (without enamel) should be at least 1.2 gram

Item should be hallmarked on the reverse of the emblem (not on pin)

Pins should have a minimum of 0.50 microns gold plating applied to assembled pin.

Epoxy resin colour should be applied to main emblem.

Base metal rubber inserted pin protector should be fitted to the end on each piece
Silver Gilt Pendant

Emblem dimensions: minimum size 17mm long x 15mm long x 1.2mm thick.

Minimum weight 1.4 gram

Chain dimensions: 20" silver trace chain approx 1 gram in weight.

Pendant to be connected to chain by way of Silver bail.      
Pendant should be hallmarked on the reverse of the emblem

Epoxy resin colour should be applied to main emblem.

Chain, bail and pendant to be gold electroplated to a minimum of 0.50 microns

Silver Pin

Emblem dimensions: minimum size 12mm long x 7.5mm long x 1.2mm thick

Stem dimensions: minimum 45mm long x .9mm thick

Pin stem to be silver soldered to emblem

Minimum weight of finished product (without resin and pin protector) should be at least 1.2 gram

Item should be hallmarked on the reverse of the emblem (not on pin)

Epoxy resin colour should be applied to main emblem.

Base metal rubber inserted pin protector should be fitted to the end on each piece

Silver Pendant

Emblem dimensions: minimum size 17mm long x 15mm long x 1.2mm thick.

Minimum weight 1.4 gram

Chain dimensions: 20" silver trace chain approx 1 gram in weight.

Pendant to be connected to chain by way of Silver bail. 
Pendant should be hallmarked on the reverse of the emblem

Epoxy resin colour should be applied to main emblem.
All items to be boxed in presentation box as per Specification PDF, please note Box must allow for the Award to be seen through lid
Please note samples (including box) must be returned prior to the closing date for receipt of tenders. No refund can be made for the cost of manufacturer. The samples of the successful supplier will be used as the template and the quality benchmark for all future supplies.

